## Slide 1: THE TEXTILE CLEANING PROCESS
CHARLES L. RIGGS, Ph.D.
Texas Woman’s University

## Slide 2: The Textile Cleaning Process

## Slide 3: The Textile Cleaning Process

## Slide 4: The Textile Cleaning Process

## Slide 5: The Textile Cleaning Process
Drycleaning Machine

## Slide 6: The Textile Cleaning Process
Wetcleaning Machine and Dryer

## Slide 7: The Textile Cleaning Process
Expectations
Remove soils and stains
Avoid damage to the item

## Slide 8: The Textile Cleaning Process
Cleaning Fluid Options
An aqueous solvent that, chemically, is a polar solvent
  Water
A nonaqueous solvent that, chemically, is a nonpolar solvent
  Currently includes petroleum and tetrachloroethylene

## Slide 9: The Textile Cleaning Process
Solvent
Odor retention
Embellishment damage, especially some types of beads and sequins
Water
Shrinkage
Color loss
Bleeding
Change in surface character
Observed Damage

## Slide 10: The Textile Cleaning Process
Relaxation
Based on how fabric has been processed or worn
Fiber is elongated
Does not recover
Relaxed by washing
Shrinkage stops when fiber is fully relaxed
Progressive
Fiber is not compatible with a specific treatment causing an irreversible shortening of the fiber
Shrinkage continues and is cumulative based on amount of exposure
Shrinkage

## Slide 11: The Textile Cleaning Process
Soils
Removed by agitation
Dissolved in water or solvent
  Polar (water soluble) includes salts, sugars, blood, urine, and other bodily fluids
  Nonpolar (solvent soluble) includes oils, greases, fats, waxes
  Particulate (not soluble) includes sand, dust, soot
Stains
Material bound in the fabric that must be modified and/or removed with chemical treatments
Attempted before cleaning, during cleaning (prespotted), or after cleaning (post spotted)
Soils and Stains

## Slide 12: The Textile Cleaning Process
Dryclean
No problem with nonpolar soils
Problem with polar soils
  Add detergents and water to the solvent (up to 75% RH)
  Pre/post spot with water
Knowledge of soil type present necessary for success
Wetclean
No problem with polar soils
Problem with nonpolar soils
  Add special detergents, emulsifiers, etc.
  Pre/post spot with solvents
Knowledge of soil type present necessary for success
Matching Cleaning Method to Soil

## Slide 13: The Textile Cleaning Process
Process developed in the 1800s
  Quality of solvent was poor, but recycling was standard practice
  No method for disposal of dirty solvent and removed soils – typically poured on the ground
    Same as for used motor oil and industrial solvents
  Problem water-soluble soils were removed by hand wetcleaning
Remediation is underway
Environmental Issues with Drycleaning

## Slide 14: The Textile Cleaning Process
Fiber can be elongated, recovery is slow
Recovery accelerated by humidity
Fiber is covered with scales that provide both positive and negative attributes
  Felting occurs when fiber is exposed to heat, moisture, and agitation
    Fiber shortens with scales overlapping and locking in position
    Narrow end of one fiber moves out of yarn structure and entangles with adjacent fiber
Wool Shrinkage

## Slide 15: The Textile Cleaning Process
Textile Fibers

## Slide 16: The Textile Cleaning Process
Dryclean
Regular cycle regardless of solvent
Local hand wetcleaning is normal procedure based on soil type
Wetclean
Mild detergent
Minimum mechanical action
Relaxation and minor felting can be recovered by elongation
Shrinkage progressive with multiple cleanings
Traditional Wool Fabrics

## Slide 17: The Textile Cleaning Process
Limited success
Partially removes the scale structure and/or coats the scales with a finish
Potential Issues
  Changes the feel (or hand) of the fabric
  Degrades the durability of the finish
  Alkali found in standard laundry detergents attacks the wool protein
Washable Wool Fabrics

## Slide 18: The Textile Cleaning Process
Dryclean
No connection to water or sewer
All solvent, soils, and additives captured, filtered, distilled
Solvent reused in same machine
Approx. 1 gallon of solvent lost for every 1000 lbs. cleaned
Wetclean
Water, removed soils, detergents discharged to sewer
Fresh water at 85˚ F to 104˚ F with consumption usually 2.4 gallons of water/lb.
Detergents based on soil and fabric type
Current Technology

## Slide 19: The Textile Cleaning Process
Washing and wetcleaning use water treated for drinking and discharge soils, detergents, solvents, and used water to the sewer
Dry-to-dry drycleaning uses solvents that are recycled by filtration and distillation
  Soils and detergents concentrated and disposed by licensed hazardous waste company
Environmentally Friendly?

## Slide 20: The Textile Cleaning Process

## Slide 21: The Textile Cleaning Process
Workwear that is heavily soiled with oil, grease, perspiration, and particulate soils
Problem for all technologies to clean
Commonly processed in industrial laundries that use water and special additives
  Discharge waste water to an onsite pretreatment plant before discharge to sewer
Scenario to Consider

## Slide 22: The Textile Cleaning Process

## Slide 23: The Textile Cleaning Process
Tunnel Washer

## Slide 24: The Textile Cleaning Process
Could dryclean with no additives to remove oil, grease and most of the particulates.
  Solvent and soils go directly to distillation
After complete solvent recovery, items are washed using water and small amount of detergent to aide in wetting
  Waste is concentrated and goes to appropriate recycle/waste disposal
  Very little is discharged with the waste water to the sewer

## Slide 25: The Textile Cleaning Process